Imprinting layer preparation

+ BHF dip

+ Spinning of mr-I 7030R

Spinning: 3000 rpm gives apx. 280nm

Soft bake: 60sec@110C