|  |
| --- |
| Objective |
| Batch name: Process template |
| This process flows is a guideline on how to use ESPACER on top of CSAR6200 e-beam resist. |

|  |  |  |  |
| --- | --- | --- | --- |
| Step Heading | Equipment |  | Comments |
| 1. Pretreatment
 |  |
| * 1. Surface treatment
 | BHF dip *or*HMDS | BHF dip for Si substrates (30 sec, H2O 5 min) HMDS treatment for SiO2 and III-V substrates | Generally, pre-treatment is not recommended.  |
| 1. Spin coat of ZEP
 |  |
| * 1. Coat wafers
 | Spin Coater | **Resist:** CSAR 6200**Spin:** 60 sec @ 4000 rpm (~180 nm)**Softbake:** 1 min @ 150 °C (hotplate) | Use syringe with filter or disposable pipette (cleaned by N2 gun). Softbake is not a crucial step according to AllResist |
| 1. Coat with ESPACER (only for non-conductive substrates)
 |  |
| * 1. Coat with ESPACER
 | Spin Coater: Manual All Purpose | **Spin:** 60 sec @ 4000 rpm**No Softbake** | Spun on like resist, no bakingEspacer is stored in the refrigerator in Cx1 |
| 1. E-beam exposure
 |  |
| * 1. E-beam exposure
 | E-beam writer | Dose: 200 - 350 µC/cm2; a dose-test is required. See e-beam logbook for inspiration. | Dose depends strongly on substrate material, thickness of resist, critical dimension and load of pattern. |
| 1. Removal of ESPACER
 |  |
| * 1. Removal of ESPACER
 | Petribowl, fumehood in C-1 or D-3 | Rinse in H2OBlow dry with N2. |  |
| 1. Development & Rinse
 |  |
| * 1. Develop-ment
 | Petribowl, fumehood in D-4 | Develop with AR 600-546, 60 secRinse in IPA, 60 secblow dry with N2 |  |
| 1. Lift-off and Strip
 |  |
| * 1. Lift-off
 | Petribowl, fumehood in D-4 | Remover 1165 in petribowl. |  |