## Slide 1
Recipe | HBr etch
HBr flow | 10 sccm
CH4 flow | 5 sccm
Ar flow | 2 sccm
Platen power | 50 W
Coil power | 600 W
Pressure | 1 mTorr + 3 s at 5 mTorr (strike) (previously used 5 mTorr)
Platen chiller temperature | 180 °C
Comment | Sample placed on 2” InP wafer crystalbonded to 4” Si carrier
HBr-based recipe for InP-based III-V materials
Recipe | Cl2/H2 etch
Cl2 flow | 6.6 sccm
H2 flow | 5.4 sccm
Ar flow | 0 sccm
Platen power | 150 W
Coil power | 800 W
Pressure | 0.5 mTorr + 10 s at 10 mTorr (strike) (throttle valve fully open, pressure limited to ~0.75 mTorr)
Platen chiller temperature | 180 °C
Comment | Sample placed on 2” InP wafer crystalbonded to 4” Si carrier
Cl2-based recipe for InP-based III-V materials

## Slide 2
“HBr etch (low p)”, tetch = 2 min
“InP Cl-H2 coil power 800”, tetch = 50 s
HSQ
InP
HSQ
InP
100 nm lines:

## Slide 3
“HBr etch (low p)”, tetch = 2 min
“InP Cl-H2 coil power 800”, tetch = 50 s
500 nm lines:
HSQ
InP
HSQ
InP

## Slide 4
“HBr etch (low p)”, tetch = 2 min
“InP Cl-H2 coil power 800”, tetch = 50 s
700 nm lines:
HSQ
InP
HSQ
InP

## Slide 5
“HBr etch (low p)”, tetch = 2 min
“InP Cl-H2 coil power 800”, tetch = 50 s
1 µm lines:
InP
HSQ
InP

## Slide 6
“HBr etch (low p)”, tetch = 2 min
“InP Cl-H2 coil power 800”, tetch = 50 s
1 µm lines, 300 nm gap:
InP
HSQ
InP

## Slide 7
“HBr etch (low p)”, tetch = 2 min
“InP Cl-H2 coil power 800”, tetch = 50 s
1 µm lines, 1 µm gap:
InP
HSQ
InP

## Slide 8
“HBr etch (low p)”, tetch = 2 min
“InP Cl-H2 coil power 800”, tetch = 50 s
“Particles” of unknown origin:
“Particles”
“Particles”
Seen such “particles” before, they seem to appear randomly sometimes.