## Slide 1: PVD co-sputter/evaporation Cryofox, Polyteknik
Deposition of
thin layers
Sputtering
E-beam
Co-sputtering
Co-ebeam

## Slide 2: Sputter sources
Quartz crystals for thickness measurement
Valve to cryopump
E-beam source 1
E-beam source 2
Shielding against cross contamination

## Slide 3: Options and sputter processes:
Options:
Sputter processes so far
2,4 or 6” wafers
Up to 24x 4” wafers…
Load lock, short pump time
Heating of wafers
Cleaning or wafers with plasma (RF clean)
Sputter targets
Al, Si, ITO, SiO2, Ni, Ag
(With higher rates, less uniform layers).
Material | Uniformity | Rate
Al | +/- 2% | ~ 1 Å/s
Si | +/- 2% | ~ 0.5 Å/s
Al+ Si | +/- 5% | ~ 1 Å/s
AlxNy | +/- 4% | ~ 0.3 Å/s

## Slide 4
Material | Uniformity | Rate
Ti | +/- 4% | ~ 2 Å/s
Al | +/- 4% | ~ 2 Å/s
Ag | +/- 3% | ~ 2 Å/s
Ni+Cr* | +/- 3% | ~ 3 Å/s
Ti+Al |  | ~ 3 Å/s
E-beam processes
E-beam processes so far
*Ni/Cr stochiometric relationship stable (about 55% Ni, 45% Cr) through the film.
Example Al +Ti
3 depositions with 3 different rates for Al and Ti
Wafer 1: 58% Al, 42% Ti
Wafer 2: 74% Al, 26% Ti
Wafer 3: 96% Al, 4% Ti